TONG  MING  ENTERPRISE  CO., LTD

| PURCHASER: | MECSU JOINT STOCK COMPANY | CERT NO： | 965712 | Report Code： |
| --- | --- | --- | --- | --- |
| ADDRESS： | 39 Tran Hung Dao Street, |  |  |  |
|  |  | CUST P/N： | D0127B3T1X0P0800 | PO# NO： |

Tan Thanh Ward,Tan Phu

District,        Ho Chi Minh

City, Vietnam

| SIZE： | M8 | MATERIAL TYPE： | A2(304) | ITEM NO: | 94457 |
| --- | --- | --- | --- | --- | --- |
| MARKING： | NO MARK | SHIP QTY： | 30000 PC | HEAT NO: | S241114AA20 |
| MFR.： | TONG MING ENTERPRISE CO.,LTD. |  |  |  |  |
|  |  | COMMODITY: | DIN127-1987 | LOT NO： | C20250402W741 |
| MFR.DATE： | 2025/03/27 |  |  |  |  |
|  |  | Product Name: | Lock Washers Type | Surface: | Passivated |

B-SquareEnds

| Sampling Date：2025/04/02 |  | Test Date： |  |  | 2025/04/02 | Sample Plan spec： |  |  |  | ANSI/ASME B18.18 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DIMENSIONAL INSPECTIONS | (mm) | SPECIFICATION |  |  | SAMPLE STANDARD： |  |  |  |  |  |
| CHARACTERISTICS |  |  |  |  | ACTUAL RESULT |  |  |  | SAMPLE DETERMINANT |  |
| Incision width |  | 1.05 max |  |  | 1.05 |  | <---> | 1.05 | Qualified |  |
| DIMENSIONAL INSPECTIONS | (mm) | SPECIFICATION |  |  | SAMPLE STANDARD： |  |  |  | DIN127-1987 |  |
| CHARACTERISTICS |  |  |  |  | ACTUAL RESULT |  |  |  | SAMPLE DETERMINANT |  |
| INNER DIAMETER |  | 8.1 | <---> | 8.5 | 8.33 |  | <---> | 8.35 | Qualified |  |
| OUTER DIAMETER |  | 14.8 max |  |  | 14.22 |  | <---> | 14.34 | Qualified |  |
| THICKNESS |  | 1.9 | <---> | 2.1 | 2.03 |  | <---> | 2.1 | Qualified |  |
| Height |  | 4 | <---> | 4.7 | 4.16 |  | <---> | 4.26 | Qualified |  |
| MECHANICAL PROPERTIES |  | SPECIFICATION |  |  | SAMPLE STANDARD： |  |  |  | DIN127 1987 TYPE B |  |
| CHARACTERISTICS |  |  |  |  | ACTUAL RESULT |  |  |  | SAMPLE DETERMINANT |  |
| Free Height |  | 3.2 min |  |  | 3.2 | <---> |  | 3.2 | Qualified |  |

CHEMICAL COMPOSITION%

| Heat Number | C | Si | Mn | P | S | Ni | Cr | Mo | Cu | N | SAMPLE DETERMINANT |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S241114AA20 | 0.053 | 0.31 | 1.01 | 0.034 | 0.002 | 8.01 | 18.1 |  | 00 | 00 | Qualified |
|  |  |  |  |  |  |  | Xiaoyang.W |  |  |  | 2025/07/28 |

| Authorization | Verification | Sampler | Date |
| --- | --- | --- | --- |

This Lot fit the demands of EN10204 3.1 
INSPECTION RESULT:SAMPLES TESTED CONFORM TO ALL OF SPECIFICATION AS ABOVE THIS REPORT MUST NOT BE REPRODUCED EXCEPT IN FULL.

WHENEVER TESTING DISCREPANCIES ARE DETECTED OR DEPARTURES FROM DOCUMENTED POLICIES AND PROCEDURE OCCUR,THEY WILL BE SHOWN IN REMARK.

a、HRC for Screw & Bolt with partial thread;HRB(S) for Nut、Thread rod and Bolt & Screw with full thread.

| Tel： +86-573-82203125 | Fax： +86-573-82207588 | 1 | Web： www.tongming.com.cn |  |  | E-mail：export@tongming.com.cn |
| --- | --- | --- | --- | --- | --- | --- |
| ADD：88 ChangSheng RD., E.D. Zone,JiaXing,ZheJiang,China |  |  | Zip：314003 |  |  | 1 |
| Page |  |  | Toal | 1 | Page |  |

|  |  | Xiaoyang.W | {{DATE}} |
| --- | --- | --- | --- |
| Authorization | Verification | Sampler | Date |

This Lot fit the demands of EN10204 3.1

INSPECTION RESULT:SAMPLES TESTED CONFORM TO ALL OF SPECIFICATION AS ABOVE THIS REPORT MUST NOT BE REPRODUCED EXCEPT IN FULL.

WHENEVER TESTING DISCREPANCIES ARE DETECTED OR DEPARTURES FROM DOCUMENTED POLICIES AND PROCEDURE OCCUR,THEY WILL BE SHOWN IN REMARK.

a、HRC for Screw & Bolt with partial thread;HRB(S) for Nut、Thread rod and Bolt & Screw with full thread.

Tel: +86-573-82203125  Fax: +86-573-82207588  Web: www.tongming.com.cn  E-mail: export@tongming.com.cn

ADD: 88 ChangSheng RD., E.D. Zone, JiaXing, ZheJiang, China  Zip: 314003